## The MasterSeries Coating Line 
Inner Panel/Inner Frame Protector 
Mastercoat Extreme Elements Corrosion Inhibitor Concentrate (EECI) Application Instructions

Surface Preparation: Surface should be clean and free of all contamination including dirt, oil and grease. 
Remove oil or grease. Remove salt and dirt deposits using a fresh water rinse at low pressure. 
Remove pack rust, loose coating and other foreign matter.

This product can be used as a single coat system or a two coat system. When using a two coat system a "wet on wet" application method is recommended.
This can be achieved by applying one coat of Mastercoat EECI at 5-6 wet mils, let flash for two hours and apply another coat at 10 wet mils.

Equipment Airless spray - 30:1 Graco Bulldog with 3/8" I.D. high pressure line and a Graco silver gun with a .021-.024 spray tip.  Engine cleaning gun also works well.

Conventional spray - Use a DV-MBC gun or equivalent with a D fluid nozzle and a 64 air cap. 
* Note - Brush and roller application can be used as well as other spray equipment.

Recommended Uses:  As a corrosion inhibiting coating, between pieces of metal such as welded seams.  For use inside rocker panels, inner frame, and cavities where corrosion is a problem, hood and deck lid welded lips, bottoms of doors, and inside windshield posts.  Can be mixed into oil based paints as a corrosion inhibitor, 8oz. (half pint) to one gallon.  Use on threaded fasteners.  Reduce with mineral spirits for spray applications.

Can be removed with wax and grease remover from painted surfaces immediately.  Do not allow to dry.

Appearance:  Amber colored grease-type consistency
Spread Rate for one coat system: 
Recommended: Wet film thickness 11-13 mils. 
Recommended: Dry film thickness 8-10 mils. 
Sag Resistance: 60 mils. 
Coverage: 150 square feet at 8 mils Dry Film Thickness. 
Thinning: Mineral spirits. 
Mixing: Mix by hand. 
Drying times 
@ 75EF: Dust free.................60 minutes. 
Firm........................48 hours. 
Recoatability...........No maximum. 
Clean Up: Clean equipment with mineral spirits. 
Topcoats: Not normally required but may be top coated.

PM Industries, 939 Westbrook Road, West Milford, NJ  07480
1-800-833-8933
www.masterseriescoatings.com