GAS TANK REPAIR INSTRUCTIONS

Severely rusted tanks: First and foremost, knock out scale and heavy rust by putting stones or marbles in the tank and banging it around. It is not suggested using metal objects that could cause sparking. The next step is a good cleaning and etching with metal prep or rust removers. Use MASTERCOAT® METAL PREP to remove rust and treat galvanized metal. Metal Prep must be THOROUGHLY DRY.When using Mastercoat Metal Prep, sloshing this metal prep in and leaving it in overnight or as long as necessary is suggested. There is no need to neutralize Metal Prep with water. Allow Metal Prep to dry thoroughly. Pour Mastercoat® Permanent Rust Sealer into tank through sending unit and slosh around to coat inside. Stand tank on end letting it DRAIN COMPLETELY into can. LET CURE 48 HOURS BEFORE USE. THIN COATS are recommended. DO NOT ALLOW COATING TO PUDDLE. USE REMAINDER OF RUST SEALER IMMEDIATELY TO COAT OUTSIDE OF TANK OR DISPOSE OF IMMEDIATELY. DO NOT STORE OR ELSE THE LID MAY BLOW OFF.

SPECIAL NOTE: Sending unit screws should have a dab of grease on the threads and ran halfway in. Drain holes can be kept open by shoving vacuum line coated with a light film of oil to prevent clogging. After the sealer dries, simply remove the hose.

Outside leaks, pinholes, and crack seams: Mastercoat Permanent Rust Sealer is recommended for the outside of the tank. Some applications will not require removal of the tank. Area to be coated must be dry and clean. Two coats are recommended. COATING SHOULD BE DRY TO TOUCH BEFORE RECOATING OR RESEALING.

For more information and reordering, visit www.nomorerust.com. For technical assistance, please call 1-800-833-8933 M-F 9am-5pm EST.